Delivery Specification of Galleon V2 Supreme (B604)

Galleon V2 Supreme (B604) is Acid Activated Powdered Bleaching Clay Manufactured From High Quality Ca-Montmorilonite of India.

Galleon V2 Supreme (B604) is a product designed with a highly porous inner structure and high surface area is developed for adsorption of color bodies, pigment, gums and other impurities from edible and non edible oil.

Delivery - Physical & Chemical Properties:

| Properties | Unit | Range |
| --- | --- | --- |
| Moisture (2 hrs at 110°C Temp.) Fineness Passing (Through 90 µ Sieve) Residual Acidity Bleaching Efficiency (Against Galleon V2 Supreme (B604) Std) | % % %H2SO4 % | 15.0 Max. 85.0 Min. 0.2 Max. 95.0 Min. |

Bleaching Efficiency spec as per IS 1965 : 1972

Effect from Jan: 2017