Delivery Specification of Galleon V2G

Galleon V2G is Acid Activated Granular Bleaching Clay Manufactured From High Quality Ca-Montmorilonite of India.

Galleon V2G is a product designed with a highly porous inner structure and high surface area is developed for adsorption of color bodies, pigment, gums and other impurities from edible and non edible oil after desirable powder size.

Delivery - Physical & Chemical Properties:

| Properties | Unit | Range |
| --- | --- | --- |
| Moisture (2 hrs at 110°C Temp.) Residual Acidity Bleaching Efficiency (Against Galleon V2 Std) | % %H2SO4 % | 15.0 Max. 0.25 Max. 95.0 Min. |

Bleaching Efficiency spec as per IS 1965 : 1972

Effect from Jan: 2017