Typical Analysis Data of Galleon V2 Super

Galleon V2 Super is Acid Activated Powdered Bleaching Clay Manufactured From High Quality Ca-Montmorilonite of India.

Galleon V2 Super is a product designed with a highly porous inner structure and high surface area is developed for adsorption of color bodies, pigment, gums and other impurities from edible and non edible oil.

Typical Chemical Composition Data :

| Properties | Unit | Typical Data |
| --- | --- | --- |
| Silica as SiO2 Aluminum as Al2O3 Iron as Fe2O3 Titanium as TIO2 Calcium as CaO Magnesium as MgO Sodium as Na2O Potasium as K2O Sulphate as SO3 LOI (1 Hrs at 1000°C Temp) | % % % % % % % % % % | 59.2 8.50 9.47 2.72 5.18 1.13 0.19 0.62 2.80 10.18 |

Other Typical Analysis Data

| Properties | Unit | Range |
| --- | --- | --- |
| Tap Bulk Density pH (5% Suspension) Average Particle Size BET Surface Area | gm/ml ------ µ M2/gm | 0.55 to 0.65 2.5 to 4.5 26 - 32 300 to 330 |

Version: Jan.2017

.